SPECIFICATIONS

NIGROSIN ALCOHOL SOLUBLE

Synonyms:				Solvent Black 5, C.I. 50415

CAS No:				11099-03-9

Appearance:				Black Powder

Identification (IR):			To conform to structure

Absorption max			565 +/-3nm
(In Ethanol)

Effective: 02/07/11